Multi-Depth Condition Rack

Model MCR-R1-A

Multipurpose Condition Rack

Model MCR-R1-A

# Text boxes

Directors

Dr. J. P. Broomfield

Mr. K. G. Davies

BGB  Projects  Ltd

CORROSION MONITORING SYSTEMS

Use

The Multipurpose Condition Rack is designed to provide varying depth information for new structures where deterioration of the structure or initiation of corrosion is of concern or of interest.

Technical Data

MCR-R1-A is our Advanced model which collates extensive concrete and reinforcement condition information from new structures. It has been designed to provide information over a varying depth profile as Figure 1.

Figure 1

The MCR-R1-A measures the corrosion rate and steel potential at four depths CR1-CR4 as well as the main reinforcement. Resistivity is also measured over three depths R1-R3 as shown in Figure 1.  This allows the engineer to identify the penetration rates of chlorides and moisture with respect to the depth from the surface of the concrete.  An intelligent identification chip which provides a unique reference is incorporated within the MCR-R1-A military specification multipin connector and housed within a remote unit.

The MCR-R1-A utilises the following components:

·  Inert Auxiliary Element

·  Ag/AgCl/KCl(0.5M)

·  Temperature Probe

The MCR-R1-A Ag/AgCl/KCl(0.5M) sensing element together with the inert auxiliary element and temperature probe, provides the engineer with the facility to gather corrosion rate, corrosion potential, concrete resistivity and concrete temperature with the PDCS instrument meter over the varying depths.

BGB Projects Ltd.

30B Vine Road,

East Molesey

Surrey KT8 9LF, UK.

Tel/Fax +44 (0) 20 8941 6696

Email johnpbroomfield@aol.com

Installation

Prior to concrete pouring the Multipurpose Condition Rack is installed by securing the device to exposed reinforcement via heavy duty cable ties. The military specification multipin connector housing

is fixed at a convenient location on the formwork to enable surface access for future readings.

Features

- Robust Construction

- Ag/AgCl/KCl(0.5M) Reference Electrode

- Identification Chip

- Military Connector

- MDCS Instrument Compatible

- Standard 1.5m Heavy Duty Conduit Cable Protection

- Specials (on request)

Applications

- Bridge Structures

- Road Decks

- Car Parks

- Buildings

- Jetties

- Tunnels

Specification

Reference Electrode

Element type Ag/AgCl/KCl(0.5M)

Potential 15mV ±10mV v SCE (Saturated Calomel Electrode)

260mV ±10mV v SHE (Standard Hydrogen Electrode)

Drift < 3mV in 24 hours

Typically < 10mV in 20 years

Internal Resistance < 2kohm

Auxiliary Element Type – Stainless Steel

Temperature Probe    –    Platinum Resistance
 		      Stainless Steel Sheath

Element PT100 BS 1904 Class B

Tolerance < 0.75 deg C at 100 deg C