LPR Corrosion Rate Meter

Model MDCS

# Text boxes

Directors

Dr. J. P. Broomfield

Mr. K. G. Davies

BGB  Projects  Ltd

CORROSION MONITORING SYSTEMS

Use

The hand held Linear Polarisation Resistance (LPR) corrosion rate

meter model MDCS is use to carry out measurements of corrosion rate of steel reinforcement in concrete from embedded

LPR probes.

Technical Data

The MDCS meter is housed in a IP65 enclosure (120 x 200 x 75mm and weighs approximately 1.5kg). The MDCS meter uses the three electrode potentiostatic linear polarisation resistance (LPR) corrosion rate measurement technique.

Corrosion rate range covered by the MDCS meter is from 0.2µm/year to 5mm/year for a 100 square centimetres surface area test electrode.

The MDSC meter is a self contained battery powered instrument which provides compatibility with the LPR-P range of probes. All measurements functions are selectable using the two push buttons and a simple menu system. The MDCS meter measures the corrosion potential (Ecorr) and corrosion rate automatically by selecting the appropriate menu. The results will be displayed on the MDCS LCD screen.

The MDCS meter will read the unique electronic identification chip within the LPR-P range of probes automatically. The MDCS meter digitally measures the corrosion potential of the test electrode with respect to a reference (half cell) electrode and applies a 20mV anodic polarisation using precision potentiostat circuitry an a third, inert auxiliary electrode.

After a short period of polarisation the board measures the polarisation current and outputs a digitally generated voltage proportional to this current and hence to the corrosion rate. The polarisation is then removed and the test cell disconnected.

Features

Three electrode potentiostatic technique

Large Corrosion Rate Range

GRP Housing

Identification Chip Readable

Standard 4mm Banana Plugs

Lightweight

LCD Screen

Battery Powered

Specification

Enclosure

Dimensions

Power Supply

Operating Temperature

Range

Corrosion Potential

Corrosion Rate

Resolution

Corrosion Potential

GRP IP65

120x200x75mm

Rechargeable Batteries

-40 to 70o C

-1024 to 1024mV

Rate 0.2µm to 5mm/year

0.5mV

BGB Projects Ltd.

30B Vine Road,

East Molesey

Surrey KT8 9LF, UK.

Tel/Fax +44 (0) 20 8941 6696

Email johnpbroomfield@aol.com